ON THE THERMO-MECHANICAL CHARACTERIZATION

OF CEMENTITIOUS MORTARS EXPOSED TO HIGH TEMPERATURE

Giovanni Bianchi and Giuseppe Rossi

**32nd Cycle of the PhD Course in**

**Structural, Seismic and Geotechnical Engineering**

**Politecnico di Milano**

Keywords: compartmentation, fire walls, mortars, hollow concrete blocks, integrity, insulation, resistance.

**Introduction**

Compartmentation is one of the key aspects in Fire Engineering, as it prevents – or limits - fire spreading to adjacent rooms. A proper fire compartmentation guarantees that the consequences of a fire are not disproportionate with respect to the fire itself; from this point of view, compartmentation is a sort of extension of the concept of *robustness*, that is a key concept in modern Structural Engineering.

A typical barrier to fire spreading is represented by fire-resistant walls, consisting of hollow clay bricks or concrete blocks and mortar joints. The typical fire performance that a load-bearing or non load-bearing wall should guarantee is a combination of integrity (E Criterion about the ability to prevent the passage of flames, hot gases and smoke from the *hot* side to the *cold* side of the wall), and insulation (I Criterion about the ability to keep the temperature rise at the *cold* side below specified levels) [1]. Clearly, the overall fire performance of a wall is controlled by the properties of the two component materials, i.e. clay bricks or concrete blocks, and mortar (in the joints).

Some recent technical documents on fire-resistant load-bearing and non load-bearing walls are bringing to the stage the thermo-mechanical behavior of the mortars, whose thin layers should not be the weakest link in a wall system, in terms of heat transfer, integrity and mechanical resistance. Information on mortars decay at high temperature, however, can hardly be found in the technical-scientific literature.

**Experimental program**

Within this context, the thermo-mechanical characterization of three mortars in *residual* conditions (i.e. past a cycle at high temperature) is presented in this paper. The first mortar (M5) is an ordinary mortar (*reference* mortar, fc ≥ 5 MPa), while the second and third mortars (M10 and M15) are high-performance/high-strength mortars (fc ≥ 10 MPa and fc ≥ 15 MPa, respectively). All mortars are tested in compression and in tension by bending in virgin conditions and past a single high-temperature cycle at 200, 400 and 600°C.

Since the focus of this research project is on the fire performance of the walls made of hollow concrete blocks, the behavior of the mortars is systematically compared with that of concrete, represented by the provisions of Eurocode 2 [2].

**Test results**

In terms of thermal properties (Figure 1a), the three mortars exhibit a thermal diffusivity significantly lower than that of ordinary concrete (from -25 to -40%). This is a plus, since in a wall the mortar joints unavoidably act as a thermal bridge (because of their continuity from the *hot* side to the *cold* side).

As for the mechanical properties, the two higher-grade mortars (M10 and M15) exhibit better strength properties than the lower-grade mortar M5, at all temperatures; the curves of the normalized strength, however, are not only very close among themselves, but also very close to those of ordinary concrete, up to 600°C (Figure 1b). The same applies to the elastic modulus, and to the tensile strength in bending. The similar loss of mechanical performance in the mortars and in ordinary concrete is something welcome, as the loss of integrity in a fire-exposed wall depends mainly on the differences exhibited by the mechanical properties and thermal dilation, between the concrete of the blocks and the mortar of the joints [3,4].

|  |  |
| --- | --- |
| Fig1a | Fig1b |

Figure 1. (a) Thermal diffusivity; and (b) residual normalized compressive strength.

**Concluding remarks**

The good performance of the mortars in question, in terms of insulation ability and integrity leads to the conclusion that in a wall, the mortar joints do not represent the *weakest link*; moreover, the good insulating properties (= low thermal diffusivity) indicate that mortars may be efficiently used in the fire protection of FRP plates, jackets and ribbons.

**Outlook**

The 3D behavior of highly-confined mortars (as in the horizontal joints of masonry structures, where mortar layers are placed between contiguous brick layers) is still an open issue, that will be treated in the continuation of this research project.

**References**

* 1. EN 1992-1-2 (2004). Design of Concrete Structures – Part 1-2: General Rules – Structural Fire Design*. Eurocode 2*, Brussels (Belgium), 97 p.
  2. Hilsdorf, H. (1965). Die Bestimmung der Zweiachsigen Festigkeit des Betons (On the Determination of Concrete Bi-Axial Strength). *Deutscher Ausschuss für Stahlbeton.* V. 173, Beuth Verlag (Berlin, Germany), pp. 000-000.
  3. Hendry A.W., Sinha B.P. and Davis S.R. (1981). An introduction to load bearing brickwork design, *Ellis Horwood* (London, U.K.), 300 p.
  4. Regan P.R. and Kennedy Reid I.L. (2009). Assessment of Concrete Structures Affected by Cover Delamination – Part 1: Effect of Bond Loss. *Studies and Researches – Annual Review of Structural Concrete,* ed. by Politecnico di Milano and Italcementi, V. 29, pub. by Starrylink (Brescia, Italy), pp. 245-275.
  5. Belletti B., Muttoni A., Ravasini S. and Vecchi F. (2019). Parametric analysis on punching shear resistance of reinforced-concrete continuous slabs. *Magazine of Concrete Research*, V.71, No.20, pp. 1083-1096.
  6. [Minkwan Ju](https://www.ncbi.nlm.nih.gov/pubmed/?term=Ju%20M%5BAuthor%5D&cauthor=true&cauthor_uid=30960819), [Kyoungsoo Park](https://www.ncbi.nlm.nih.gov/pubmed/?term=Park%20K%5BAuthor%5D&cauthor=true&cauthor_uid=30960819) and [Cheolwoo Park](https://www.ncbi.nlm.nih.gov/pubmed/?term=Park%20C%5BAuthor%5D&cauthor=true&cauthor_uid=30960819) (2018).Punching Shear Behavior of Two-Way Concrete Slabs Reinforced with Glass-Fiber-Reinforced Polymer (GFRP) Bars**.** *Polymers (Basel)*, pub. on-line 9 August 2018, doi: [10.3390/polym10080893](https://dx.doi.org/10.3390%2Fpolym10080893)
  7. Dönmez A. and Bažant Z. (2017). Size Effect on Punching Strength of Reinforced Concrete Slabs with and without Shear Reinforcement. *ACI – Structural Journal*, V. 114, No. 4, pp. 875-886.
  8. Trekin N. and Pekin D. (2019). Experimental research on punching shear mechanisms in reinforced concrete slabs. *Proc. XXII Int. Scientific Conf. “Constructions and the Formation of Living Environment – FORM 2019”* , Paper No. 04032, 12 p., (<https://doi.org/10.1051/e3sconf/20199704032>).

P.S.:

* authors should stress – even concisely – the original/innovative aspects of their thesis, and the possible short/medium/long-term applications of their results/models/theories.
* British and American English (both permitted) should not be mixed-up.
* The long abstracts (max. 4 pages) text may be subdivided into a number of sections (Introduction with the objectives and the outline of the research project, theoretical/numerical model or experimental program, main numerical/experimental results, conclusions/concluding remarks, outlook and references).